TimberForm Specifications

# No. 5107 Leg-Flex Station

FITNESS EQUIPMENT

Fitness station shall be a TimberForm( No. 5107 Leg-Flex as manufactured by Columbia Cascade Company, 1300 SW Sixth Avenue, Suite 310, Portland OR 97201-3464 U.S.A.

GENERAL

Leg-Flex station shall consist of three posts at graduated heights and one instructional sign manufactured in accordance with the following quality and design standards.  All fabrication shall take place in an enclosed factory environment by personnel experienced in the manufacture of fitness equipment.

1.0  SIGNAGE

1.1  Instructional Sign

Instructional sign shall consist of a wood frame and graphic panel.

Frame timbers shall be free-of-heart-center, kiln dried C and better Douglas fir.  There shall be no loose knots nor knotholes.  To eliminate slivering, timbers shall be free of wane, precision milled to pattern, smoothly dressed four sides to a net size of 3-3/8 inch x 5-3/8 inch (86 mm x 137 mm) and have their edges and ends heavily eased.  After fabrication, timbers shall be preservatively treated with a non-toxic formulation capable of deep penetration without materially changing the color of the wood to which it is applied.  Sign posts shall be treated in accordance with Section 5.0 and notched at the top and middle to accept similarly-notched horizontal timbers.

Sign frame shall be factory-assembled with 1 inch (25 mm) diameter wooden dowel permanently secured with exterior grade wood glue.  After assembly, any excess dowel shall be trimmed flush with the surface of the frame and sanded smooth.  The graphic panel shall be permanently recessed within its assembled sign frame.

Graphic panel shall be fabricated of 18 gauge (1.2 mm) mild steel plate and include a graphic illustration and written instructions for safe and proper use of the fitness apparatus.  Panel shall be porcelain enamel finished BLUE or GREEN with white graphics in accordance with Paragraph 1.3.

1.3  Signage Finish

Graphic panel shall be finished on all sides with porcelain enamel, a colorful, glossy, tough, extremely weather-resistant finish.  The porcelain enamel process shall permanently fuse a thick layer of glass to the metal substrate at temperatures exceeding 1,500(F (815(C).  To assure adhesion, only glasses possessing thermal expansion qualities lower than those of the steel plate shall be accepted.

2.0  FITNESS STATION

2.7  Leg-Flex

Posts shall be 6 x 6 (nominal) in accordance with Section 5.0.  Instructional sign shall be in accordance with Section 1.0.

5.0  TIMBER MATERIALS

All fitness equipment wood components shall be manufactured from Playground Equipment Grade Douglas fir timbers, selected by the equipment manufacturer for strength, durability, and appearance.

5.1  Playground Equipment Grade

Timber posts and platforms shall be Coastal Douglas fir (Pseudo-tsuga menziesii), free-of-heart-center (F.O.H.C.).  To assure long, useful life, timbers containing the heart center or pith of the log shall not be accepted.

5.2  Timber Characteristics

All timbers shall be fine-grained, with at least 80 percent of the pieces possessing eight annular rings to the inch, the remainder having at least six rings to the inch.  There shall be no loose knots, knotholes, shake, unsound wood, white specks or honeycomb allowed.  To eliminate slivering, timbers shall be free of wane, and planer skips are not allowed in dressing.  Except as noted, other characteristics and limiting provisions are in accordance with Paragraph 131-A Standard Grading Rules for West Coast Lumber.

5.3  Chronological Importance

To effectively receive pressure preservative treatment of the timber materials, all fabrication, including sawing, notching, drilling, incising and kerfing, shall be completed prior to preservative treatment.

5.4  Wood Preservation

All wood components shall be pressure-preservatively treated with a water repellant formulation designed for use on fitness equipment.  Preservatives containing arsenic, pentachlorophenol, creosote or similar toxic chemicals as their active ingredient shall not be used.

5.4.1  Composition

The preservative solution shall be homogeneous and capable of deep penetration, not merely an emulsion.  The treatment shall not materially change the color of the wood to which it is applied.

5.4.2  Application

Wood shall be pressure impregnated by the closed cylinder, vacuum pressure method as prescribed by the latest standards for the American Wood Preservers' Association.  The preservative carrier shall conform to AWPA Standard C1 (latest edition).

5.4.3  Verification

Accordance to the requirements of this specification shall be monitored by an independent inspection agency in accordance with established industry quality control and inspection procedures.

5.4.4  Max-Treat( - Incising

Timber posts shall be mechanically incised on all four faces by uniform hydraulic pressure to a depth of 1/2 inch (13 mm).  Incising shall begin at the bottom of the post and end approximately one foot (305 mm) above grade.  Full length incising is not acceptable as the perforations may cause slivering of timber surfaces.  The incising pattern shall produce a minimum of 448 perforations per square foot (929 cm2).

5.4.5  Max-Treat - Kerfing

All timber posts shall be saw-kerfed (grooved) to one-half the cross-section depth, through sap-side face.  This kerf shall be a maximum of 1/4 inch (6 mm) wide and shall extend from the bottom of the post to  a point approximately one foot (305 mm) above indicated grade, coincident with incising.

Incising and kerfing assure maximum wood preservative penetration and retention in the critical ground line area thus assuring long service life.

5.5  Posts

Timber posts shall be smoothly dressed to a net size of 5-1/4 inch x 5-1/4 inch (133 mm x 133 mm) with all edges eased (rounded) to a 1/4 inch (6 mm) radius.  Post tops shall be chamfer-sawn 45 degrees.

5.6  Quality Control

Inspectors shall examine each timber component for correct fabrication, fastener hole alignment, and for smooth end, edge, and face treatment.

7.0  INSTALLATION INSTRUCTIONS AND AIDS

To guide installation, each No. 5107 Leg-Flex station shall be accompanied by bills of materials, written instructions, and erection drawings to be furnished prior to or with the delivery of the fitness equipment.  To facilitate assembly, each part shall be indelibly stenciled with an easily-read identification number keyed to the bills of materials and erection drawings. All components shall be shipped unitized, protectively wrapped, banded for mechanical handling and ready for assembly.