TimberForm Specifications

# No. 5113 Sit-Up Station

FITNESS EQUIPMENT

Fitness station shall be a TimberForm( No. 5113 Sit-Up as manufactured by Columbia Cascade Company, 1300 SW Sixth Avenue, Suite 310, Portland OR 97201-3464 U.S.A.

GENERAL

Sit-Up station shall consist of two front rails, one rear support, two timber seats and one instructional sign manufactured in accordance with the following quality and design standards.  All fabrication shall take place in an enclosed factory environment by personnel experienced in the manufacture of fitness equipment.

1.0  SIGNAGE

1.1  Instructional Sign

Each introduction sign shall consist of a wood frame and graphic panel.

Frame timbers shall be free-of-heart-center, kiln dried C and better Douglas fir.  There shall be no loose knots nor knotholes.  To eliminate slivering, timbers shall be free of wane, precision milled to pattern, smoothly dressed four sides to a net size of 3-3/8 inch x 5-3/8 inch (86 mm x 137 mm) and have their edges and ends heavily eased.  After fabrication, timbers shall be preservatively treated with a non-toxic formulation capable of deep penetration without materially changing the color of the wood to which it is applied.  Sign posts shall be treated in accordance with Section 5.0 and notched at the top and middle to accept similarly-notched horizontal timbers.

Sign frame shall be factory-assembled with 1 inch (25 mm) diameter wooden dowel permanently secured with exterior grade wood glue.  After assembly, any excess dowel shall be trimmed flush with the surface of the frame and sanded smooth.  The graphic panel shall be permanently recessed within its assembled sign frame.

Graphic panel shall be fabricated of 18 gauge (1.2 mm) mild steel plate and include a graphic illustration and written instructions for safe and proper use of the fitness apparatus.  Panel shall be porcelain enamel finished BLUE or GREEN with white graphics in accordance with Paragraph 1.3.

1.3  Signage Finish

Graphic panel shall be finished on all sides with porcelain enamel, a colorful, glossy, tough, extremely weather-resistant finish.  The porcelain enamel process shall permanently fuse a thick layer of glass to the metal substrate at temperatures exceeding 1,500(F (815(C).  To assure adhesion, only glasses possessing thermal expansion qualities lower than those of the steel plate shall be accepted.

2.0  FITNESS STATION

2.13  Sit-Up

Seat slats shall be 3 x 8 (nominal) in accordance with Section 5.0.  Front rails shall be curved  1-5/8" (o.d.) schedule 40 mild steel pipe.  Rear Support shall be curved 2-3/8" (o.d.) schedule 40 mild steel pipe.  Seat frames shall be 1-5/8" (o.d.) schedule 40 mild steel pipe and 1/4” thick mild steel plate.  Front rails, rear support and seat frames shall be manufactured in accordance with Section 3.0 and CASPAX-7 finished in accordance with Section 4.0.  Instructional sign shall be in accordance with Section 1.0.

3.0  METAL MATERIALS

Except as noted, all pipe rails shall be schedule 40 steel pipe in accordance with ASTM A-53, Type E, Grade A.  Thin wall tubing is not acceptable.  Steel plate shall be in accordance with ASTM A-36.  All steel parts shall be CASPAX-7( finished in accordance with Section 4.0.

3.1  Fabrication

All welds are to comply with AWS standard D1.1.  All edges, ends, and welds shall be ground smooth by hand to a maximum grit of 36 and shotblasted to a uniform surface texture.

3.2  Quality Control

Inspectors shall examine metal components for correct fabrication, fastener hole alignment, and smoothness.

3.3  Additional Hardware

Additional hardware shall be provided in sufficient quantity to complete assembly of the TimberForm Fitness Station.  All hardware shall be non-ferrous, color finished with CASPAX-7, galvanized, or electrostatic zinc plated in accordance with the manufacturer's standard.

4.0  METAL FINISH

Metal parts, except fasteners and sign panels, shall be finished with CASPAX-7, a colorful, tough, opaque, exterior use powder coating.  Liquid, epoxy, or lead-containing powder coatings are not acceptable.  The CASPAX-7 color shall be the manufacturer's standard or as selected by the owner's representative and designated on the project plans and/or specifications.

4.1  Cleaning

Substrate preparation shall consist first of mechanical cleaning to remove heavy mill scale, rust, varnish, grease, etc., then chemical cleaning in accordance with TT-C-490C, Methods I and III.

4.2  Phosphate Application

After cleaning, the metal substrate shall receive a corrosion-inhibiting iron phosphate coating in accordance with TT-C-490C, Type II, before application of the final color coat.

4.3  Powder Application

The coating powder shall be uniformly applied by the electrostatic method to a minimum thickness of six mils.  Promptly after the application of the powder, the coating shall be oven-cured at 400(F (204(C) to chemically bond the finish to the substrate and to render the color finished surface resistant to abrasion, impact, household chemicals, weathering and rusting.

4.4  Chronological Importance

For a corrosion-inhibiting agent to be effective, all fabrication including cutting, coping, grinding, and welding must be completed before application of the corrosion-inhibiting agent.  Corrosion-inhibiting agents applied prior to fabrication are not acceptable.

4.5  Quality Control

The applicator shall test the finish of each lot for correct millage, chemical resistance,  hardness, and internal bond in accordance with established industry standard test methods.

Records of this quality control procedure shall be made and retained for two years.

5.0  TIMBER MATERIALS

All fitness equipment wood components shall be manufactured from Playground Equipment Grade Douglas fir timbers, selected by the equipment manufacturer for strength, durability, and appearance.

5.1  Playground Equipment Grade

Timber posts and platforms shall be Coastal Douglas fir (Pseudo-tsuga menziesii), free-of-heart-center (F.O.H.C.).  To assure long, useful life, timbers containing the heart center or pith of the log shall not be accepted.

5.2  Timber Characteristics

All timbers shall be fine-grained, with at least 80 percent of the pieces possessing eight annular rings to the inch, the remainder having at least six rings to the inch.  There shall be no loose knots, knotholes, shake, unsound wood, white specks or honeycomb allowed.  To eliminate slivering, timbers shall be free of wane, and planer skips are not allowed in dressing.  Except as noted, other characteristics and limiting provisions are in accordance with Paragraph 131-A Standard Grading Rules for West Coast Lumber.

5.3  Chronological Importance

To effectively receive pressure preservative treatment of the timber materials, all fabrication, including sawing, notching, drilling, incising and kerfing, shall be completed prior to preservative treatment.

5.4  Wood Preservation

All wood components shall be pressure-preservatively treated with a water repellant formulation designed for use on fitness equipment.  Preservatives containing arsenic, pentachlorophenol, creosote or similar toxic chemicals as their active ingredient shall not be used.

5.4.1  Composition

The preservative solution shall be homogeneous and capable of deep penetration, not merely an emulsion.  The treatment shall not materially change the color of the wood to which it is applied.

5.4.2  Application

Wood shall be pressure impregnated by the closed cylinder, vacuum pressure method as prescribed by the latest standards for the American Wood Preservers' Association.  The preservative carrier shall conform to AWPA Standard C1 (latest edition).

5.4.3  Verification

Accordance to the requirements of this specification shall be monitored by an independent inspection agency in accordance with established industry quality control and inspection procedures.

5.4.4  Max-Treat( - Incising

Timber posts shall be mechanically incised on all four faces by uniform hydraulic pressure to a depth of 1/2 inch (13 mm).  Incising shall begin at the bottom of the post and end approximately one foot (305 mm) above grade.  Full length incising is not acceptable as the perforations may cause slivering of timber surfaces.  The incising pattern shall produce a minimum of 448 perforations per square foot (929 cm2).

5.4.5  Max-Treat - Kerfing

All timber posts shall be saw-kerfed (grooved) to one-half the cross-section depth, through sap-side face.  This kerf shall be a maximum of 1/4 inch (6 mm) wide and shall extend from the bottom of the post to  a point approximately one foot (305 mm) above indicated grade, coincident with incising.

Incising and kerfing assure maximum wood preservative penetration and retention in the critical ground line area thus assuring long service life.

5.5  Posts

Timber posts shall be smoothly dressed to a net size of 5-1/4 inch x 5-1/4 inch (133 mm x 133 mm) with all edges eased (rounded) to a 1/4 inch (6 mm) radius.  Post tops shall be chamfer-sawn 45 degrees.

5.6  Quality Control

Inspectors shall examine each timber component for correct fabrication, fastener hole alignment, and for smooth end, edge, and face treatment.

6.0  OPTIONAL BENCH MATERIAL

Benches are optionally available with SofDek( coated perforated steel seats.

6.2  SofDek( Perforated Steel Benches

Benches shall be manufactured of 11 gage (.125" thick) perforated mild steel plate.  Each unit shall be reinforced with 1/4 inch thick mild steel bar as necessary to insure structural integrity. No sharp metal edges shall be exposed.  Benches shall be thermoplastic coated in accordance with Paragraph 6.2.3.

6.2.1 Cleaning

Substrate preparation shall consist first of mechanical cleaning to remove heavy mill scale, rust, varnish, grease, etc., then chemical cleaning in accordance with TT-C-490C, Methods I and III.

6.2.2 Phosphate Application

After cleaning, the metal substrate shall receive a corrosion-inhibiting iron phosphate coating in accordance with TT-C-490C, Type II, before application of the final color coat.

6.2.3 Thermoplastic Application

The ultra-violet stabilized thermoplastic coating shall be applied by the electrostatic process to pre-heated substrate to a thickness of approximately 30 mils then allowed to cure before handling.  Final Durometer (hardness) shall be 52 on the D Shore scale in accordance with ASTM D 2240.  The color finished surface shall bond to the substrate and be resistant to abrasion, impact, household chemicals, weathering and rusting.

6.2.4 Chronological Importance

For a corrosion-inhibiting agent to be effective, all fabrication including cutting, coping, grinding, and welding must be completed before application of the corrosion-inhibiting agent.  Corrosion-inhibiting agents applied prior to fabrication are not acceptable.

6.2.5 Quality Control

The applicator shall test the finish of each lot for correct millage, chemical resistance, hardness, and internal bond in accordance with established industry standard test methods.  Records of this quality control procedure shall be made and retained for two years.

7.0  INSTALLATION INSTRUCTIONS AND AIDS

To guide installation, each No. 5113 Sit-Up station shall be accompanied by bills of materials, written instructions, and erection drawings to be furnished prior to or with the delivery of the fitness equipment.  To facilitate assembly, each part shall be indelibly stenciled with an easily-read identification number keyed to the bills of materials and erection drawings. All components shall be shipped unitized, protectively wrapped, banded for mechanical handling and ready for assembly.