TimberForm Specifications

# No. 5107-R Leg-Flex Station w/Recycled Plastic Posts

FITNESS EQUIPMENT

Fitness station shall be TimberForm( No. 5107-R Leg-Flex as manufactured by Columbia Cascade Company, 1300 SW Sixth Avenue, Suite 310, Portland OR 97201-3464 U.S.A.

GENERAL

Leg-Flex station shall consist of three posts at graduated heights and one instructional sign manufactured in accordance with the following quality and design standards.  All fabrication shall take place in an enclosed factory environment by personnel experienced in the manufacture of fitness equipment.

1.0  SIGNAGE

1.1  Instructional Sign

Instructional sign shall consist of pipe frame and graphic panel.

One piece pipe frame shall be 1-5/16" (33 mm) o.d. schedule 40 steel pipe formed into a "U" shape.  Each frame leg shall embed 3'-0" (915 mm) below finished grade and have a 9/16" diameter hole to receive one No. 4 reinforcing bar (to be supplied by installing contractor).  Pipe frame shall be ground smooth, deburred, and CASPAX-7( finished in accordance with Section 4.0.

Sign panel shall be fabricated of 18 gauge (1.2 mm) mild steel plate and include a graphic illustration and written instructions for safe and proper use of the fitness apparatus.  Panel shall be porcelain enamel finished BLUE or GREEN with white graphics in accordance with Paragraph 1.3.  The manufacturer shall attach panels to sign frames with vandal-resistant fasteners.

1.3  Signage Finish

Graphic panel shall be finished on all sides with porcelain enamel, a colorful, glossy, tough, extremely weather-resistant finish.  The porcelain enamel process shall permanently fuse a thick layer of glass to the metal substrate at temperatures exceeding 1,500(F (815(C).  To assure adhesion, only glasses possessing thermal expansion qualities lower than those of the steel plate shall be accepted.

2.0 FITNESS APPARATUS

2.7  Leg-Flex

Posts shall be 6 x 6 (nominal) in accordance with Section 5.0.  Instructional sign shall be in accordance with Section 1.0.

5.0  HDPE RECYCLED PLASTIC MATERIALS

All fitness equipment plastic timber components shall be 100% post-consumer extruded HDPE, cedar colored, selected by the equipment manufacturer for strength, durability and appearance.  Molded recycled plastic timbers have unacceptable surface texture and shall be rejected.

5.1  Posts

Posts shall be smoothly extruded to a net size of 5-1/4 inches x 5-1/4 inches with all edges eased (rounded).  Post tops shall be chamfer-sawn 45 degrees on four faces.

5.3  TimGrip™ Fasteners

TimGrip stainless steel bolts are furnished as standard.  TimGrip hardware has unique thread geometry especially designed, tested and proven to securely and permanently grip recycled HDPE plastic.  Ferrous or ordinary lag screw fasteners shall not be accepted for HDPE connections.

5.4  Quality Control

Inspectors shall examine each component for correct fabrication, fastener hole alignment, and for smooth end, edge, and face treatment.

5.6  Quality Control

Inspectors shall examine each component for correct fabrication, fastener hole alignment, and for smooth end, edge, and face treatment.

7.0  INSTALLATION INSTRUCTIONS AND AIDS

To guide installation, each No. 5107-R Leg-Flex station shall be accompanied by bills of materials, written instructions, and erection drawings to be furnished prior to or with the delivery of the fitness equipment.  To facilitate assembly, each part shall be indelibly stenciled with an easily-read identification number keyed to the bills of materials and erection drawings. All components shall be shipped unitized, protectively wrapped, banded for mechanical handling and ready for assembly.