TimberForm Specifications

# No. 5112 Vault-Over Station

FITNESS EQUIPMENT

Fitness station shall be TimberForm( No. 5112 Vault-Over as manufactured by Columbia Cascade Company, 1300 SW Sixth Avenue, Suite 310, Portland OR 97201-3464 U.S.A.

GENERAL

No. 5112 Vault-Over station shall consist of a vaulting rail and instructional sign manufactured in accordance with the following quality and design standards.  All fabrication shall take place in an enclosed factory environment by personnel experienced in the manufacture of fitness equipment.

1.0  SIGNAGE

1.1  Instructional Sign

Instructional sign shall consist of a wood frame and graphic panel.

Frame timbers shall be free-of-heart-center, kiln dried C and better Douglas fir.  There shall be no loose knots nor knotholes.  To eliminate slivering, timbers shall be free of wane, precision milled to pattern, smoothly dressed four sides to a net size of 3-3/8 inch x 5-3/8 inch (86 mm x 137 mm) and have their edges and ends heavily eased.  After fabrication, timbers shall be preservatively treated with a non-toxic formulation capable of deep penetration without materially changing the color of the wood to which it is applied.  Sign posts shall be treated in accordance with Section 5.0 and notched at the top and middle to accept similarly-notched horizontal timbers.

Sign frame shall be factory-assembled with 1 inch (25 mm) diameter wooden dowel permanently secured with exterior grade wood glue.  After assembly, any excess dowel shall be trimmed flush with the surface of the frame and sanded smooth.  The graphic panel shall be permanently recessed within its assembled sign frame.

Graphic panel shall be fabricated of 18 gauge (1.2 mm) mild steel plate and include a graphic illustration and written instructions for safe and proper use of the fitness apparatus.  Panel shall be porcelain enamel finished BLUE or GREEN with white graphics in accordance with Paragraph 1.3.

1.3  Signage Finish

Graphic panel shall be coated on all sides with porcelain enamel, a colorful, glossy, tough, extremely weather-resistant finish.  The porcelain enamel process shall permanently fuse a thick layer of glass to the metal substrate at temperatures exceeding 1,500(F (815(C).  To assure adhesion, only glasses possessing thermal expansion qualities lower than those of the steel plate shall be accepted.

2.0  FITNESS STATION

2.12  Vault-Over

Curved vaulting rail shall be 1-5/8" (o.d.) schedule 40 steel pipe manufactured in accordance with Section 3.0 and CASPAX-7 coated in accordance with Section 4.0.  Instructional sign shall be in accordance with Section 1.0.

3.0  METAL MATERIALS

Except as noted, all pipe rails shall be schedule 40 steel pipe in accordance with ASTM A-53, Type E, Grade A.  Thin wall tubing is not acceptable.  Steel plate shall be in accordance with ASTM A-36.  All steel parts shall be CASPAX-7( finished in accordance with Section 4.0.

3.1  Fabrication

All welds are to comply with AWS standard D1.1.  All edges, ends, and welds shall be ground smooth by hand to a maximum grit of 36 and shotblasted to a uniform surface texture.

3.2  Quality Control

Inspectors shall examine metal components for correct fabrication, fastener hole alignment, and smoothness.

3.3  Additional Hardware

Additional hardware shall be provided in sufficient quantity to complete assembly of the TimberForm Fitness Station.  All hardware shall be non-ferrous, color finished with CASPAX-7, galvanized, or electrostatic zinc plated in accordance with the manufacturer's standard.

4.0  METAL FINISH

Metal parts, except fasteners and sign panels, shall be finished with CASPAX-7, a colorful, tough, opaque, exterior use powder coating.  Liquid, epoxy, or lead-containing powder coatings are not acceptable.  The CASPAX-7 color shall be the manufacturer's standard or as selected by the owner's representative and designated on the project plans and/or specifications.

4.1  Cleaning

Substrate preparation shall consist first of mechanical cleaning to remove heavy mill scale, rust, varnish, grease, etc., then chemical cleaning in accordance with TT-C-490C, Methods I and III.

4.2  Phosphate Application

After cleaning, the metal substrate shall receive a corrosion-inhibiting iron phosphate coating in accordance with TT-C-490C, Type II, before application of the final color coat.

4.3  Powder Application

The coating powder shall be uniformly applied by the electrostatic method to a minimum thickness of six mils.  Promptly after the application of the powder, the coating shall be oven-cured at 400(F (204(C) to chemically bond the finish to the substrate and to render the color finished surface resistant to abrasion, impact, household chemicals, weathering and rusting.

4.4  Chronological Importance

For a corrosion-inhibiting agent to be effective, all fabrication including cutting, coping, grinding, and welding must be completed before application of the corrosion-inhibiting agent.  Corrosion-inhibiting agents applied prior to fabrication are not acceptable.

4.5  Quality Control

The applicator shall test the finish of each lot for correct millage, chemical resistance,  hardness, and internal bond in accordance with established industry standard test methods.

Records of this quality control procedure shall be made and retained for two years.

7.0  INSTALLATION INSTRUCTIONS AND AIDS

To guide installation, each No. 5112 Vault-Over station shall be accompanied by bills of materials, written instructions, and erection drawings to be furnished prior to or with the delivery of the fitness equipment.  To facilitate assembly, each part shall be indelibly stenciled with an easily-read identification number keyed to the bills of materials and erection drawings. All components shall be shipped unitized, protectively wrapped, banded for mechanical handling and ready for assembly.