TimberForm Specifications

# No. 5120-02 Post with Directional Arrow

TimberForm( No. 5120-02 Post with Directional Arrow shall be as manufactured by Columbia Cascade Company, 1300 SW Sixth Avenue, Suite 310, Portland OR 97201-3464 U.S.A.

1.0  General

Post shall be shall be 5-1/4 inch x 5-1/4 inch (133 mm x 133 mm) manufactured in accordance with Section 5.0 and include a 1/4 inch (6 mm) deep recess for directional graphic disk.   Each disk shall be 3-1/2" (102 mm) in diameter and fabricated of 20 gauge (1.2 mm) mild steel plate.  Disks shall be porcelain enamel finished BLUE or GREEN with white arrow in accordance with Section 3.0.

2.0  Construction

Disk shall be oriented by installing contractor and secured with two vandal-resistant screws.  Directional sign post placement and orientation shall be as selected by the project architect or owner.

3.0  Sign Panel Finish

Graphic panel shall be finished on all sides with porcelain enamel, a colorful, glossy, tough, extremely weather-resistant finish.  The porcelain enamel process shall permanently fuse a thick layer of glass to the metal substrate at temperatures exceeding 1,500(F (815(C).  To assure adhesion, only glasses possessing thermal expansion qualities lower than those of the steel plate shall be accepted.

5.0  HDPE RECYCLED PLASTIC MATERIALS

Post shall be 100% post-consumer extruded HDPE, cedar colored, selected by the equipment manufacturer for strength, durability and appearance.  Molded recycled plastic timbers have unacceptable surface texture and shall be rejected.

5.1  Posts

Post shall be smoothly extruded to a net size of 5-1/4 inches x 5-1/4 inches with all edges eased (rounded).  Post tops shall be chamfer-sawn 45 degrees on four faces.

5.4  Quality Control

Inspectors shall examine each component for correct fabrication, fastener hole alignment, and for smooth end, edge, and face treatment.

5.6  Quality Control

Inspectors shall examine each component for correct fabrication, fastener hole alignment, and for smooth end, edge, and face treatment.